VAG BAIO®plus System
VAG NOVA 284 Standpost Hydrant
PN 16 - DN 80 / 100
Possible connections: flange or spigot

Product features
• Design type AUD and AFUD (DN 100) acc. to DIN 3222
• DN 100 optional without A extraction
• Safety lock of the inner function unit
• Automatic draining and pressure water protection
• Maintenance-free stem seal with O-rings in brass bushings
• Free orientation of the hydrant

Materials and corrosion protection
• Upper and lower column of ductile cast iron EN-JS 1050 (GGG-50)
• Head (AUD) and cover (AFUD) of aluminium alloy
• Valve cone of EN-JS 1050 (GGG-50), EPDM vulcanised
• Bonnet and couplings size A / B of aluminium alloy
• Inside true enamel, outside prime enamel, epoxy coating
• Colour: RAL 3000 / flame red
• Elastomers approved acc. to W 270
• Approved and registered by DVGW

Field of application
• Water distribution / water supply