Double-socket locking part 
PN 16
DN 100 ... 150 
for easy assembly (disassembly) of the BAIO®plus System 
or the pipeline. 
Designed as
- divisible pipe coupling,
- split BAIO-U part with externally lockable centre piece,
- with double-function socket on both sides according to DIN 28603 for the positive, tensile-load resistant interior locking with BAIO®plus System parts as well as for the exterior locking of cast-iron and plastic pipes.
Entirely made of EN-JS 1030 (GGG-40) ductile cast iron 
Application area: drinking water 
Max. operating pressure: water 16 bar 

Corrosion protection:	inside and outside 
			epoxy coating,
			RAL 5005 blue, 

e.g. VAG BAIO®DVS Double-socket lock

Pc ........   Euro/Pc .........   Euro/Item .........