EU-part 
PN 16
DN 80 ... 200
made of ductile iron EN-JS 1030 (GGG-40),
with double-function socket on one side,
for positive direct interior interlocking 
with BAIO® plus System parts and for
exterior interlocking of cast-iron and plastic pipes,
socket designed for sealing ring to DIN 28 603,
with flange connection on the other side,
flange connection dimensions- to DIN EN 1092.
Corrosion protection:	inside and outside
			epoxy coating
			blue, RAL 5005
			
e.g. VAG BAIO®EU-part

Pc ........   Euro/Pc.........   Euro/Item .........