Gate Valve PN 16
for BAIO®plus System, tension proof,
DN 80...300,
Flanged connection / spigot end,
Body parts made of ductile iron EN-JS 1030 (GGG-40)
with flanged connection and spigot end
for non-positive locking, direct connection 
to the BAIO®plus System,
continuous pipe culvert,
boltless cover,
with inside screw,
wedge vulcanised all over with EPDM, with wedge drainage,
wedge rubber coating approved to KTW and W 270,
stem made of stainless steel with min. 13 % Cr,
maintenance-free stem seal
(O-rings inserted in brass bushing),
Corrosion protection:	inside and outside
				epoxy coating,
				blue, RAL 5005
				to GSK guidelines

DIN-DVGW registered

e.g. 	VAG BETA® 200 Gate Valve flange/spigot for cast-iron pipes
or similar

Options:	- with VAG VA telescopic equipment
	    	  Adjustment range:	1.00 – 1.40 m
						1.20 – 1.80 m
						1.70 – 2.70 m
		- with fully enclosed position indicator

Pc ........   €/Pc .........   €/Item .........