VAG BAIO®sit
Tension protection for cast iron pipes

Produkt features
• Positive locking, exterior interlock between the spigot pipe end and the BAIO®plus-socket
• Screwless
• 2-piece design
- Tension ring of cast iron
- Clamping ring of  elastomer
• Can be easily disconnected
• Correct seat of seal can be verified while pipe is inserted

Materials and corrosion protection
• Tension ring made of ductile iron EN-JS 1030 (GGG-40)
• Clamping ring made of elastomere, NIRO hooks vulcanised onto inside, separate clamping ring

Field of application
• Water distribution / water supply