VAG Underground Hydrant
PN 10 - DN 50
PN 16 - DN 100

Product features
• Simple shut-off
• Automatic draining and pressure water protection
• Maintenance-free stem seal

Materials and corrosion protection
Version PN 10 – DN 50
• Jacket, cover and distributor head (car washing design) of cast iron EN-JL 1040 (GG-25)
• Valve cone of EN-JL 1040 (GG-25), NBR vulcanised
• Inside and outside epoxy coating

Version PN 16 – DN 100
• Jacket and valve cone of cast iron EN-JL 1040 (GG-25)
• Inlet part, outlet and cover of ductile cast iron EN-JS 1050 (GGG-50)
• Valve cone NBR vulcanised
• Inside and outside epoxy coating

Field of application
• Irrigation in agriculture, horticulture and public parks