Underground hydrant PN 16
DN 100
to DIN 3221
Body parts made of cast iron EN-JL 1040 (GG-25),
with automatic drainage,
with pressure water protection,
stem made of stainless steel with min. 13 % Cr,
maintenance-free stem seal,
valve cone made of EN-JL 1040 (GG-25), with EPDM coating,
pressure pipe made of stainless steel,
stem nut made of EN-JS 1050 (GGG-50),
screws with nuts made of A2 stainless steel,
flange connection dimensions to EN 1092,
Corrosion protection: 	inside and outside
		epoxy coating, 
		blue, RAL 5005 

Pipe cover: for 1.00 m, 1.25 m or 1.50 m

e.g. VAG underground hydrant DN 100

Option:  - with double shut-off

Pc ........   Euro/Pc .........   Euro/Item .........